## Slide 1: New instruments for online measurements of alkali and tars during gasification of Biomass
KENT DAVIDSSON, MOHIT PUSHP, DAN GALL, JAN PETTERSSON

## Slide 2: Background
heat
gas
tar
KOH(g), NaCl(g), …
CO2 or H2O
gas
KOH(g), NaCl(g) …
Gasification:
Tars are unwanted
Gaseous alkali affects the process
Need for online monitoring of tars and alkali

## Slide 3: Objectives
Measurements in a demo-scale gasifier (GoBiGas)
Long-term measurements
Obtain reasonable concentrations
  Calibrations
  Response to operational changes

## Slide 4: The GoBiGas gasifier

## Slide 5: Extraction
Instruments

## Slide 6: Surface Ionisation
Hot surface
e-
The process of an atom being
ionised upon desorbtion from a
surface.
Alkali specific
+

## Slide 7: Surface Ionisation Detector (SID)
A – Grounded detector plate
B – Hot platinum filament, +400 V
Simple and robust technique

## Slide 8: Alkali and particles
Startup and shutdown of GoBiGas:
An submicron particle instrument and the SID connected to the extraction system.
Measurement for two days.

## Slide 9: Scanning Mobility Particle Sizer
Fluidisation off
Fluidisation on
Feedstock
Startup

## Slide 10: SID step response
Alkali concentrations during addition of K2CO3:

## Slide 11: Alkali Aerosol Mass Spectrometer (Alkali AMS)
11
3. Time-of-flight mass spectrometer
1. Aerosol inlet (aerodynamic lens system)
2. Particle vaporisation and surface ionization (hot surface)
ions
inlet
Box-like Pt surface at 1500 K

## Slide 12: Alkali AMS
Olivine addition
Potassium concentration measured with Alkali AMS Total alkali concentration measured with SID

## Slide 13: Volatility Tandem Differential Mobility Analyser (VTDMA)
KCl
KOH
Tar
NaOH
NaCl
Aerosol

## Slide 14: VTDMA
Exp. 1
Exp. 2
Exp. 3
Thermal stability of particles

## Slide 15: Conclusions
Calibrated long-term measurements have for the first time been carried out with two alkali instruments and two particle instruments.
Thermal stability (VTDMA) has been used to analyse alkali and tars.
The methods are promising for online monitoring of large-scale gasification processes.