## Slide 1: Suitable additives for activation of olivine
Pavleta Knutsson, Chalmers

## Slide 2: Why indirect biomass gasification?
available and CO2 neutral alternative for production of multiple raw materials
heat needed for the endothermic process is assured without gas mixing

## Slide 3: Indirect gasification bottlenecks
Increased cost with gas cleaning (tars can condensate and cause clogs)
Unplanned stops (agglomerates can cause defluidization)
tar formation
Bed agglomeration
Alternative bed material:
Catalytic
Low agglomeration tendency

## Slide 4: Gasifier– black box?
Fuel
Bed material in
Bed material out
Fluidization steam
Raw gas
Improved tar yield and as a result improved quality of the product gas
Still unknown mechanism

## Slide 5: Bed material interactions
SiO2
Al2O3
(Mg,Fe)2SiO4
Agglomeration = unwanted
Activation = wanted
Agglomeration = unplanned operation stops
Activation = Increased efficiency of the process

## Slide 6: Why invest more research in bed material?
Chart: Publications about bed material and gasification
| 1966 | 1970 | 1973 | 1974 | 1975 | 1976 | 1977 | 1978 | 1979 | 1980 | 1981 | 1982 | 1983 | 1984 | 1985 | 1986 | 1987 | 1988 | 1989 | 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017
Antal publikationer | 13 | 20 | 25 | 22 | 13 | 9 | 8 | 7 | 20 | 7 | 13 | 18 | 19 | 17 | 23 | 25 | 17 | 17 | 20 | 30 | 33 | 38 | 38 | 18 | 19 | 17 | 23 | 17 | 25 | 17 | 30 | 17 | 33 | 38 | 38 | 51 | 44 | 97 | 104 | 62 | 76 | 89 | 104 | 103 | 110 | 115 | 140
vs.
vs.
Bed material changes leads to improved activity
Increase in the questions stated – increased amount of the answers reached

## Slide 7: Bed material activity
Formation of coating coupled with bed material activity
Formation of agglomerates coupled with K
Unknown precise content of the coating

## Slide 8: Experimental conditions
Chalmers Unit
GoBiGas Unit
Different operational conditions and different pre-treatment of bed material
Common activation aimed with addition of K2CO3

## Slide 9: Methodology within the project
Analysis:
Gas
Tar
Bed material
Based on gas and tar measurements – defined bed sampling
Bed morphology and chemical content of ”active materials”
K2CO3

## Slide 10: Bed material before exposure - inactive
Even distribution and dense material – Chalmers case
Porous structure and Fe-segregations – GoBiGas case

## Slide 11: Chalmers case – gas and tar analysis
Benzene and one aromatic ring compounds - major tars, all tars influenced upon activation
H2/CO ratio of 2.4 upon activation (1.14 inactive)
Decrease in CH4 , decrease in CO and increase in CO2 and H2

## Slide 12: GoBiGas case – gas and tar analysis
Benzene and two and more aromatic rings- major tars, all tars influenced upon activation
H2/CO ratio of 1.72 (2.4 upon activation in Chalmers, 1.14 - inactive)
Lower levels of CH4 – lower reforming, similar case of WGS as Chalmers

## Slide 13: Activity of bed materials
Chalmers (non-active) <GoBiGas(non-active) < GoBiGas(activated) < Chalmers (activated).

## Slide 14: Active bed material – Chalmers case
Ca-layer formed around the particles
Mixed Ca and K layer with Ca/K > 10

## Slide 15: Active bed material – GoBiGas case
Ca-layer formed around the particles
Mixed Ca and K layer with Ca/K layer close to 5

## Slide 16: Deactivated bed material – GoBiGas case
Ca-layer formed around the particles
K enrichments predominantly within the particles
Ca/K ratio of more than 20

## Slide 17: Ca, K – phases within particles
Leachability of K can be r elated to activity
CaFeO2 can be identified as the K-bearing phase

## Slide 18: Mechanism of activation and deactivation
Only surface enrichments of K can lead to an activeity of the material
When separate phases formed – loss of activity

## Slide 19: Conclusions
Two different units tested – Chalmers, GoBiGas
Two olivine materials with differen pre-treatments can lead to the similar activation result
Combined effect of Ca and K observed
By adding K2CO3– response in the tar content
All tars influenced by the selected activation

## Slide 20: Future work
What is the role of the Ca-formed phase for activity in the presence of K2CO3?
What is the role of the layer build-up for the activity? How is Ca, K –layer built and what is the influence on the model tars? (DFT)
Stability and control of the stability of the activated layer – natural migration?

## Slide 21
Thank you for your attention!