## Slide 1
Wheat straw as a material in co-digestion with other nitrogen-rich substrate
Swarnima Agnihotri Swedish Centre for Resource Recovery
University of Borås
Sweden

## Slide 2: Introduction
Project aims to investigate the co-digestion process using straw pellets or briquettes along with food waste

## Slide 3: Straw products
Raw straw
Better utilization of agricultural by-products
Straw briquettes and pellets
Established and manageable
straw products
    High C/N
Low concentrations of trace elements, limit microbial growth and activity
Suitable for co-digestion!
Straw briquettes
Straw pellets

## Slide 4: Straw as stabilizing substrate
Investigation of the value of straw as a codigestion material to other nitrogen-rich substrate
Partners: JTI, SLU, TechnoFarm, Laga Bioenergi
C/F Nielsen, Borås Energy and Environment
Straw should have positive effects like:
Balanced C/N
Activation of cellulose-degrading bacteria
Better utilization of reactor volume
Increased productivity

## Slide 5: Work plan
Characterization of straw pellets and briquettes:
Compositional analysis of straw
Straw crystallinity and structural changes (due to pelleting or briquetting) by FTIR and Simon’s staining
Continuous digestion experiments in lab scale
Digestion process (thermophilic at 55 °C) was monitored by measuring the following parameters:
Methane yield
Process stability (pH, VFA accumulation, VFA/Alkalinity ratio)
Presence and activity of cellulose degrading microbes

## Slide 6: Results so far…

## Slide 7: Compositional analysis of straw pellets and briquettes
Parameters | Straw pellets | Straw briquettes
Water soluble extractives, % | 7.65 | 6.57
Ethanol soluble extractives, % | 1.14 | 3.25
Total extractives, % | 8.79 | 9.82
Ash, % | 1.08 | 0.87
Lignin and holocellulose percentage after extractive and ash correction in whole biomass |  | 
Acid insoluble lignin, % | 17.5 | 16.4
Acid soluble lignin, % | 6.47 | 6.25
Total lignin, % | 24.0 | 22.66
Holocellulose, % (100- (Total Ext. + Ash+ Total lignin)) | 66.13 | 66.65

## Slide 8: Via FTIR eyes:

## Slide 9: Batch digestion: methane yield

## Slide 10: Continuous digestion at HB

## Slide 11: Increased loading/OLR
Addition of straw started vid OLR of 3gVS/L/d FW
GO1: Reference, only FW
GO2: + 10% straw
GN1: + 20% straw

## Slide 12: Description of used mixtures of wheat straw (either straw pellets or briquettes) and food waste in the study
Food waste (FW) | Reactor | Wheat straw (WS) (pellets or briquettes) | Comment
FW | R1 | No WS | Only FW added to the reactor at a certain OLR (between 0.5-7 g VS L-1 d-1)
FW | R2 | +10% extra VS from WS | FW added at a certain OLR (same as in R1 fed with only FW) with an addition of 10% more VS L-1 d-1 by adding WS
FW | R3 | +20% extra VS from WS | FW added at a certain OLR (same as in R1 fed with only FW) with an addition of 20% more VS L-1 d-1 by adding WS

## Slide 13
Addition of straw pellets/methane yield

## Slide 14: Addition of straw pellets/productivity

## Slide 15: Digestate characteristic: pH in reactors (Slightly alkaline, which is desirable) Digestate characteristics are relevant for its use as fertilizer

## Slide 16: Digestate characteristic: FOS/TAC (Volatile fatty acids/total inorganic carbonate)
Guide value of assessing fermentation
process 0,5-0,6 = excessive biomass input 0,4-0,5 = Plant is heavily loaded 0,3-0,4 = Biogas production is
at maximum 0,2-0,3 = Biomass input is low <0,2 = Biomass input is far too low

## Slide 17: Digestate characteristic: Substrate degradation rate (Pellets)

## Slide 18: Mechanical problems with briquettes!
+20% admixture of straw briquettes
It had built up a crust that seemed to consist of straw and 5-7 cm deep at the reactor wall and extending into 1/2 - 2/3 radius toward the centre where the agitator breaks the surface
Agitators seem to manage to keep the digester continuously mixed deeper into the digester

## Slide 19: +10% Straw briquettes
Picture of surface of the CSTR which has 10% admixture of straw briquettes
Also in this digester sometimes built up a smaller crust which appeared to consist of straw
It was about 1-2 cm deep at the reactor wall and extended into about 1/5 radius toward the centre where the agitator breaks the surface

## Slide 20
Addition of briquettes/Methane production
GO1 reference, only FW
GO2 + 10% straw
GN1 + 20% straw

## Slide 21
GO1 reference, only FW
GO2 + 10% straw
GN1 + 20% straw
Addition of briquettes/Productivity

## Slide 22
GO1 reference, only FW
GO2 + 10% straw
GN1 + 20% straw
VFA

## Slide 23: Simon’s staining: mg dye/g fibre
Chart: 
| Virgin straw | Pellets | Briq | 10% Briq | 20% Briq | 10% Pellets | 20% Pellets
Adsorbed Orange dye | 13.1121 | 28.1606 | 20.1247 | 94.8873 | 56.0211 | 91.828 | 92.1387
Adsorbed Blue dye | 24.9061 | 33.7312 | 19.4942 | 5.983 | 11.878 | 0.8625 | 0.88548

## Slide 24: Conclusions
Higher methane productivity in reactors with straw
Simon’s staining suggest that straw had become more porous and had been well digested by microbes specially pellets
OLR up to 7 gVS/L/d for FW and up to 8,4 gVS/L/d with addition of straw
HRT around 15.5 days
VFA accumulation in all reactors with increasing loading with straw briquettes
Microbial investigations to be carried out

## Slide 25: Thank you!
Energimyndigheten
Ilona Sárvári Horváth(HB)
Maria del Pilar Castillo (JTI)
Leticia Pizzul (JTI)
Mats Edström (JTI)
Anna Schnürer (SLU)
Borås Energi och Miljö
Laga Bioenergi
C/F Nielsen
TechnoFarm